SPECIFICATION

**SIKAFLEX® AT-FAÇADE INSTALLED AS A CONNECTION JOINT BEWTEEN SUPER-STICK TAPE AND POWDER COATED OR ANODISED ALUMINIUM WINDOW AND DOOR FRAMES**

|  |  |  |  |
| --- | --- | --- | --- |
| **PROJECT NAME:** |  | | |
| **PROJECT LOCATION:** |  | | |
| **SCOPE OF WORK:** |  | | |
| **SPECIFICATION DATE:** |  | **SPECIFICATION NO.:** |  |

|  |  |
| --- | --- |
| **PRODUCTS:** | **Sikaflex AT-Facade**  **Sika Activator-250**  **Sika PEF Rod** |

***Always refer to the most current product data sheet(s) available at the date of this specification.***

1. **General.**
2. This technical specification is to be read in conjunction with the project Contract Documents and Specification.
3. All work to be carried out in accordance with the current Sika (NZ) Ltd data sheets.

**2 Outline Procedure.**

**2.1 Window Joint Configuration.**

2.1.1The joint configuration (width to depth ratio) is to be in accordance with the data sheet.

**2.2 Surface Preparation.**

2.2.1 The SUPER-STICK tape and anodised /powder coated aluminium bond surfaces must be sound, clean, dry and free from concrete laitance and any loosely adhering particles or other surface contaminants such as oil, grease, fats, chemicals, rust, paint, curing membranes, etc.

**2.3 Installation.**

2.3.1 A bond breaker tape or PEF rod is required in the base of the joint to prevent three-sided adhesion of the sealant and to control the sealant depth.

2.3.2 Using a clean dry lint free rag, wipe the bond surfaces of the powder coated /anodised aluminium window components and SUPER-STICK tape with Sika Activator-205.

2.3.3 Using a separate clean dry lint free rag immediately wipe off the Sika Activator-205 and wait 10 minutes before installing sealant.

2.3.4 Install Sikaflex AT-Façade in accordance with the data sheet.